5.0mm   INFRARED EMITTING DIODE

TYPE:KI-850X

- DIMENSIONS --- UNIT ：m/m

2.ABSOLUTE  MAXIMUM  RATINGS  AT  Ta=25℃

| Characteristic | Symbol | Rating | Unit |
| --- | --- | --- | --- |
| Pulse forward current (t10us) | IMP | 1 | A |
| Forward direct current | IFM | 100 | mA |
| Reverse voltage | VRM | 5 | V |
| Operating temperature | Topr | -25 to +75 | ℃ |
| Storage temperature | Tstg | -25 to +100 | ℃ |
| Power dissipation | Pd | 200 | mW |
| Lead soldering temperature (5mm from body ) 260℃ for 5sec. |  |  |  |

3.ELECTRO-OPTICAL  CHARACTERISTICS  AT  Ta=25℃

| Characteristic | Symbol | Condition | Min. | Typ. | Max. | Unit |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | IF=50mA | 50 | 100 |  |  |
| Forward voltage | VF | IF=100mA |  | 1.6 | 2.0 | V |
| Reverse current | IR | VR=4V |  |  | 10 | μA |
| Peak emission wavelength | λp | IF=50mA |  | 850 |  | nm |
| Spectral band width @ 50% | λ | IF=50mA |  | 42 |  | nm |
| Rise time/Fall time | tr/tf | IF=50mA |  | 25/15 |  | ns |
| Viewing angle | 2θ 1/2 | IF=50mA |  | 30 |  | deg. |

5.0mm   INFRARED EMITTING DIODE

TYPE:KI-850X

5.0mm   INFRARED EMITTING DIODE

TYPE:KI-850X

5.0mm   INFRARED EMITTING DIODE

TYPE:KI-850X

CONDITIONS：

The reliability of products shall be satisfied with items listed below.

| NO. | # Item | Condition | Time/Cycle | Number of Damaged |
| --- | --- | --- | --- | --- |
| 1 | Soldering Heat Test | 260℃ | 5 sec | 0/60 |
| 2 | Thermal Shock | 0℃(15sec) ~100℃(15sec) | 20 cycle | 0/60 |
| 3 | High Temp. Storage | 100℃ | 1000 Hrs | 0/60 |
| 4 | Low Temp. Storage | -25℃ | 1000 Hrs | 0/60 |
| 5 | Operation Temperature Cycle Test | -25℃~75℃ | 100 Cycles, 200Hrs | 0/60 |
| 6 | High Temp. High Humidity Test | 60℃, 90% RH | 1000Hrs | 0/60 |
| 7 | Operation Life Test | Room Temp.50mA | 1000Hrs | 0/60 |

佳皇科技有限公司

KOODYZ Technology Co., Ltd

http://www.led-shop.com.tw