##### PHOTO TRANSISTOR 光 電 晶 體

Part Number: KO-TNS151

Package outlines

NOTES:

- All dimensions are in millimeters (inches);

2. Tolerances are 0.1mm (0.004inch) unless otherwise noted.

RECOMMEND PAD LAYOUT

| ITEM | MATERIALS |
| --- | --- |
| Resin (mold) | Epoxy |
| Bonding Wire |  30 m Au |
| Lens color | Water transparent |
| Printed circuit board | BT (white) |
| Dice | Silicon |

| ##### PHOTO TRANSISTOR 光 電 晶 體 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Part Number: KO-TNS151 |  |  |  |  |  |  |  |
| Absolute maximum ratings (TA=25℃) |  |  |  |  |  |  |  |
| Parameter | Symbol | Value |  |  |  | Unit |  |
| #### Power dissipation | PD | 100 |  |  |  | mW |  |
| #### Collector-emitter voltage | VCEO | 30 |  |  |  | V |  |
| #### Emitter-collector voltage | VECO | 5 |  |  |  | V |  |
| #### Operating temperature range | TOP | -20 ~+80 |  |  |  | ℃ |  |
| Storage temperature range | TSTG | -20 ~+80 |  |  |  | ℃ |  |
| Electro-optical characteristics (TA=25℃) |  |  |  |  |  |  |  |
| ## Parameter | # Test Condition | Symbol | Value |  |  |  | ## Unit |
|  |  |  | Min | Typ | Max |  |  |
| Collector-emitter breakdown voltage | # IC = 100µA I B= 0 | # BV CEO | 10 | -- | -- |  | V |
| Emitter-collector breakdown voltage | # IE= 100µA # I B= 0 | # BVECO | 5 | -- | -- |  | V |
| Collector dark current | # VCE = 10V H = 0mW/cm2 | # ICEO | -- | -- | 100 |  | nA |
| Collector-emitter saturation voltage | # IC=2 mA I B=100µA | # VCE (S) | -- | -- | 0.3 |  | V |
| Current gain | # VCE = 5V IC=2mA | # hFE | 200 | -- | -- |  | -- |

7-2

Soldering iron Basic spec is  5sec when 260℃. If temperature is higher, time should be shorter (+10℃ -1sec ).Power dissipation of iron should be smaller than 20W, and temperatures should be controllable .Surface temperature of the device should be under 230℃ .  Reflow Temp/Time Rework - Customer must finish rework within 5 sec under 260℃. - The head of iron can not touch copper foil - Twin-head type is preferred. NOTES: - We recommend the reflow temperature 245℃(±5℃).the maximum soldering temperature should be limited to 260℃. - dont cause stress to the epoxy resin while it is exposed to high temperature. - Number of reflow process shall be 2 times or less.  Avoid rubbing or scraping the resin by any object, during high temperature, for example reflow 、solder etc.

7-3

7-4  Handling precautions 1. Over-current-proof Customer must apply resistors for protection; otherwise slight voltage shift will cause big current change (Burn out will happen). 2.Storage 2.1 It is recommended to store the products in the following conditions: Humidity: 60% R.H. Max. Temperature : 5℃~30℃(41℉~86℉) - Shelf life in sealed bag: 12 month at ＜5℃~30℃ and ＜30% R.H. after the package is Opened, the products should be used within a week or they should be keeping to stored at ≦20 R.H. with zip-lock sealed. 3.Baking It is recommended to baking before soldering when the pack is unsealed after 72hrs. The Conditions are as followings: 3.1 60±3℃ x(12~24hrs) and ＜5%RH, taped reel type 3.2 100±3℃ x(45min~1hr), bulk type 3.3 130±3℃ x(15~30min), bulk type

| ##### PHOTO TRANSISTOR 光 電 晶 體 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| ##### Test items and results of reliability |  |  |  |  |  |
| Type | Test Item | Test Conditions | Device Hours/Cycle | Device # Tested | # Failures |
| 1 | Temperature Cycle | # -20℃ 30min # 50min↑↓100min 80℃ 30min | 50 cycle | 22 | 0 |
| 2 | Thermal Shock | # -20℃ 15min # ↑↓ 80℃ 15min | 50 cycle | 22 | 0 |
| 3 | High Temperature High Humidity Test | Ta=85℃ RH 85% | 1000 hrs | 22 | 0 |
| 4 | High Temperature Storage | Ta=80℃ | 1000 hrs | 22 | 0 |
| 5 | Low Temperature Storage | Ta= -30℃ | 1000 hrs | 22 | 0 |
| 6 | DC Operating Life | VCE = 5V Ta= 25℃ Ee=1mW/cm2 | 1000 hrs | 22 | 0 |